## Slide 1
Biogenic synthesis of Silver nanoparticles from Oldenlandiya Corymbosa plant extract and their antimicrobial activity for wound dressing application
K S Deepak
Under guidance of Dr. Bimal Das
Department of Chemical Engineering
National Institute of Technology, Durgapur -713209, India

## Slide 2
Background
Motivation
Why
01
Materials
Methods
How
02
Results & Discussion
Conclusion
What
03
Contents

## Slide 3
Introduction
1
Green synthesis of AgNPs over conventional methods

## Slide 4
Various Methods of AgNPs synthesis
AgNO3
Nano Silver
Physical Methods
Chemical Methods
Green Methods

## Slide 5
Physical Methods
Radiolytic Synthesis
Photochemical Process
Chemical Methods
Turkevich method
Green Methods
Laser ablation
Brust method
Seeded growth method
Utilization of microorganisms
Use of plants and plant extracts
Use of templates like membranes and viruses DNA
Energy extensive
Source:- Tran and Le, 2013
Toxic and non-ecofriendly byproducts
Source:- Ahmed et al. 2016
Source:- Reddy et al. 2012

## Slide 6
Introduction
1
2
Green synthesis of AgNPs over conventional methods
Use of AgNPs in Wound dressing applications over antibiotics WRT diabetic patients

## Slide 7
India is the “World Capital of diabetes”
One in six people with diabetes in the world is from India

## Slide 8
1 in every 11 person in the world is having diabetes & responsible for 60% of all limb amputations
Diabetes & Limb amputations
80% of all limb amputation in diabetic people is due to foot ulcer & wounds
Foot Ulcer & wounds
Unbridled use of antibiotics may lead to highly resistant bacterial populations
Antibiotic resistance
Source:- IDF Diabetes Atlas, 9th edn
Source:- Choudhury et al. 2020
Source:- Mosselhy et al. 2017
New therapeutic modalities that are less likely to promote bacterial resistance
Source:- Hajipour et al. 2012; Strohal et al. 2005; Stryjewski et al. 2014
AgNPs has less tendency to elicit bacterial resistance
Source:- Parani et al. 2016

## Slide 9
1
2
Green synthesis
Wound dressing
Vision & Motivation

## Slide 10
Materials
Oldenlandia corymbosa

## Slide 11
Oldenlandia corymbosa
Source:- Das et al. 2019; Noiarsa et.al, 2008
Anti-microbial
Anti-inflammatory
Anti-diabetic
Source:- Archana et al. 2021; Permawati et al. 2019
Flavonoids
Alkaloids
Phytosterols
Phenolic compounds
Steroids
Terpenoids

## Slide 12
Method
Process Flow Diagram

## Slide 13
Preparation of plant extract
Preparation of Silver Nitrate solution
Synthesis of Silver Nanoparticles

## Slide 14
Preparation of plant extract
01
Plant
Roots removed
Washed
Underwent Reflux Process
Dried for 2 days
Powdered
Mixed with distilled water
Placed on Hot plate Magnetic Stirrer
Boiled for 2 hrs
Filtered
1600C and stirrer at 400 rpm
3.3gm Powder
150ml Distilled Water

## Slide 15
Normal filter sieve
Whatman filter paper grade 41
Syringe filter of pore size 0.22 µm
Filtration
Before Filtration
After Filtration

## Slide 16
Preparation of Silver Nitrate solution
02
Deionized and Distilled water
N/10 Silver Nitrate Solution
1mM Silver Nitrate Solution
M1V1= M2V2
Operating Conditions:-
200 rpm || 15 min

## Slide 17
Preparation of AgNPs
03
Plant Extract (2ml)
Silver Nitrate solution (8ml)
Light Gold Colored Mixture
vigorous stirring
AgNPs

## Slide 18
Results and Discussion
UV- Visible Spectroscopy
Scanning Electron Microscopy Analysis
Dynamic Light Scattering study
Energy-dispersive X-ray spectroscopy Analysis
Fourier-transform infrared spectroscopy
X-ray diffraction Analysis
Characterization

## Slide 19
UV- Visible Spectroscopy
Chart: Wavelength (nm)
| 300 | 350 | 400 | 450 | 500 | 550 | 600 | 650 | 700 | 750 | 800
30 Mins | 0.218 | 0.152 | 0.156 | 0.132 | 0.079 | 0.046 | 0.033 | 0.026 | 0.022 | 0.019 | 0.016
2 Hours | 0.195 | 0.157 | 0.217 | 0.194 | 0.092 | 0.045 | 0.027 | 0.018 | 0.014 | 0.01 | 0.009
1 Day | 0.199 | 0.17 | 0.25 | 0.22 | 0.099 | 0.06 | 0.035 | 0.02 | 0.016 | 0.012 | 0.0098
3 Days | 0.207 | 0.187 | 0.316 | 0.267 | 0.14 | 0.076 | 0.042 | 0.026 | 0.018 | 0.013 | 0.01
5 Days | 0.238 | 0.243 | 0.445 | 0.364 | 0.215 | 0.113 | 0.086 | 0.056 | 0.039 | 0.028 | 0.02
Plant | 0.232 | 0.15 | 0.095 | 0.089 | 0.075 | 0.07 | 0.06 | 0.03 | 0.022 | 0.021 | 0.019
Chart: Wavelength (nm)
| 300 | 350 | 400 | 450 | 500 | 550 | 600 | 650 | 700 | 750 | 800
1P:9 | 0.2 | 0.13 | 0.138 | 0.16 | 0.085 | 0.035 | 0.025 | 0.023 | 0.018 | 0.015 | 0.011
2P:8 | 0.218 | 0.12 | 0.156 | 0.132 | 0.079 | 0.046 | 0.033 | 0.026 | 0.022 | 0.019 | 0.016
3P:7 | 0.25 | 0.18 | 0.12 | 0.078 | 0.07 | 0.05 | 0.038 | 0.03 | 0.02 | 0.018 | 0.016
4P:6 | 0.3 | 0.19 | 0.13 | 0.082 | 0.075 | 0.055 | 0.05 | 0.035 | 0.03 | 0.029 | 0.028
5P:5 | 0.4 | 0.2 | 0.135 | 0.09 | 0.08 | 0.058 | 0.055 | 0.038 | 0.04 | 0.034 | 0.032
UV-vis absorption spectrum WRT time interval
UV-vis absorption spectrum WRT mixing ratio

## Slide 20
Scanning Electron Microscopic Analysis
AgNPs
Mag= 50 KX
Mag= 75 KX
Mag= 100 KX
Before centrifugation
After centrifugation
1500 rpm || 10 min

## Slide 21
Energy Dispersive X-ray Spectroscopic Analysis
Elemental Mapping
Elemental Ag

## Slide 22
Chart: 2θ (degree)
30
50
60
70
80
90
100
(1,1,1)
(2,0,0)
(2,2,0)
(3,1,1)
(2,2,2)
38.41
44.48
64.78
77.73
81.88
X-ray Diffraction study
Reference file: JCPDS, silver file no. 04-0783
2θ | d (inter-planar spacing) | Calculation of miller indices |  |  | hkl (miller indices)
 |  | 1000/d2 | (1000/d2)/60.62 | =(h2+k2+l2) | 
2θ | d (inter-planar spacing) | Calculation of miller indices |  |  | hkl (miller indices)
 |  | 1000/d2 | (1000/d2)/60.62 |  | 

## Slide 23
Fourier transform Infrared Spectroscopic Analysis

## Slide 24
Dynamic Light Scattering study
Chart: Size (nm)
| 1.117 | 1.294 | 1.4990000000000001 | 1.736 | 2.0099999999999998 | 2.3279999999999998 | 2.6960000000000002 | 3.1219999999999999 | 3.6150000000000002 | 4.1870000000000003 | 4.8490000000000002 | 5.6150000000000002 | 6.5030000000000001 | 7.5309999999999997 | 8.7210000000000001 | 10.1 | 11.7 | 13.54 | 15.69 | 18.170000000000002 | 21.04 | 24.36 | 28.21 | 32.67 | 37.840000000000003 | 43.82 | 50.75 | 58.77 | 68.06 | 78.819999999999993 | 91.28 | 105.7 | 122.4 | 141.80000000000001 | 164.2 | 190.1 | 220.2
 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0.2 | 1.5 | 4.1 | 7.2 | 9.7 | 11 | 10.7 | 9 | 6.6 | 4 | 1.8 | 0.6 | 0.4 | 0 | 0 | 0 | 0 | 0
DLS histogram showing the size distribution
Zeta potential of AgNPs

## Slide 25
Antimicrobial evaluation
Chart: Inhibition zone (mm)
| AgNPs | AgNO3 | Plant extract | Streptomycin
E. coli | 12.3 | 10.9 | 8.4 | 23
S. aureus | 14.1 | 9.2 | 7.5 | 21
C. tetani | 11.8 | 0 | 0 | 0
S. aureus
E. coli
(d)
(a)
(c)
(b)
(d)
(a)
(b)
(c)

## Slide 26
Possible reaction mechanism
AgNO3
Plant Extract
Reductant
Capping Agent
Ag+
e-
Reductant
Ag0
e-
Reductant
Nucleation
Condensation
Surface reduction
Stabilization & Capping

## Slide 27
Cost estimation
Chart: Service providers
| Sigma-Aldrich, Inc. | SRL Pvt. Ltd. | Synthesized NPs
Cost | 383.27 | 313.9 | 115.72
Raw material cost
Raw material processing cost
Cost of reaction
Product processing cost
Total cost of AgNPs
Source:- Datta, D., Halder, G. et al. 2019

## Slide 28
S
Eco-friendly
Cost-effective
Strength
Reaction mechanism
Weakness
Wound dressing
Wound Healing
Opportunity
Cytotoxicity
Blood clotting
Scarring of Tissues
Threat
W
O
T
SWOT Analysis

## Slide 29
Promote healing
Minimal pain
Prevent infection
Minimal Scarring
Inexpensive
Easy to use
Ideal AgNPs based wound dressing

## Slide 30
Rafique, M., Sadaf, I., Rafique, M. S., & Tahir, M. B. (2017). A review on green synthesis of silver nanoparticles and their applications. Artificial cells, nanomedicine, and biotechnology, 45(7), 1272-1291.
Li, S., Shen, Y., Xie, A., Yu, X., Qiu, L., Zhang, L., & Zhang, Q. (2007). Green synthesis of silver nanoparticles using Capsicum annuum L. extract. Green Chemistry, 9(8), 852-858.
Ezeabara, C. A., & Egwuoba, G. C. (2016). Comparative screening of phytochemical and proximate constituents of leaf, stem and root of Oldenlandia corymbosa L. and Oldenlandia herbacea (L.) Roxb. American Journal of Life Science Researches, 4(3).
Archana, V., Thomas, N. N., Lakshmi, S., Rauf, A. A., & Edwin, B. T. (2020). Pharmaceutical properties of Oldenlandia corymbosa Linn. Materials Today: Proceedings.
Tran, Q. H., & Le, A. T. (2013). Silver nanoparticles: synthesis, properties, toxicology, applications and perspectives. Advances in Natural Sciences: Nanoscience and Nanotechnology, 4(3), 033001.
Reddy, G. A. K., Joy, J. M., Mitra, T., Shabnam, S., & Shilpa, T. (2012). Nano silver–a review. Int J Adv Pharm, 2(1), 09-15.
Ahmed, S., Ahmad, M., Swami, B. L., & Ikram, S. (2016). A review on plants extract mediated synthesis of silver nanoparticles for antimicrobial applications: a green expertise. Journal of advanced research, 7(1), 17-28.
References

## Slide 31
Thank You